Colloidal Processing of Alumina-Zirconia Composites
A Case Study in Modeling and Simulation Techniques applied to Colloidal Processing for Advanced Ceramic Processing Applications

Pradip

Minerals and Materials Processing Group

Tata Research Development & Design Centre 
(A Division of Tata Consultancy Services)
Pune 411 013

pradip.p@tcs.com
Abstract

Alumina-Zirconia composites are an important family of structural ceramics materials due to their high strength and toughness properties. These materials are of particular interest to us in India since we are richly endowed with excellent deposits of zircon and bauxite, the natural sources of zirconia and alumina respectively. In order to achieve better properties in the final product, colloidal processing has several advantages over conventional dry processing route. The salient findings of our research work on the colloidal processing of alumina-zirconia ceramics are presented in this colloquium. These include:

· Experimental investigations on and theoretical models for the dispersion and rheology of mixed alumina-zirconia suspensions

· Design of tailor-made dispersants based on a molecular modeling approach

· Dispersion and consolidation of concentrated alumina-zirconia suspensions in order to produce a homogeneous, defect-free green compact including determination of the extent of dispersion and modeling the role of powder size, packing, solid loading, relative proportion of the constituents and surface-colloidal properties of powders obtained from different sources

· Population balance modeling and computer-aided control of the evolution of microstructure during sintering of green compacts

___________________________________________

This research program was partially supported by Department of Science and Technology (DST) and National Institute of Standards & Technology (NIST) under the auspices of Indo-US Co-operative Research and executed in collaboration with NIST. The presentation is based on the work carried out our research group consisting of several colleagues of mine, over a period of several years. Their efforts and contributions as well as financial support from DST/NIST are gratefully acknowledged.

Key Publications from the group on this topic:
· Pradip, Beena Rai and P.Sathish, Rational Design of Dispersants by Molecular Modeling for Advanced Ceramic Processing Applications KONA, 22, 2004, pp 151-158

· Pradip, Beena Rai, P.Sathish and S. Krishnamurty, Rational Design of Dispersants for Colloidal Processing of Barium Titanate Suspensions by Molecular Modelling, Ferroelectrics , 306, 2004, pp 195-208

· M. Subbanna, P.C. Kapur and Pradip, Role of Powder Size, Packing, Solid Loading and Dispersion in Colloidal Processing of Ceramics, Ceramics International, 28(4), (2002) pp 401-405
· Pradip and Beena Rai, Design of Tailor-made Surfactants for Industrial Applications using a Molecular Modeling Approach, Colloids and Surfaces, 205(1-2), (2002) pp 139-148
· Manjunath Subbanna, P.C. Kapur and Pradip, Computer-Aided Control of the Evolution of Microstructure during Sintering, Materials Chemistry and Physics, 67(1-3), (2001) pp 17 – 24
· Subbanna, M., Kapur, P.C., Pradip and Malghan, S.G, Population Balance Model for Solid State Sintering. Part I. Pore Shrinkage and Densification, Ceramics International, 27 (1), (2001) pp 57 - 62.

· Sivakumar, S., Subbanna, M., Sahay, S.S., Ramakrishnan, V., Kapur, P.C., Pradip and Malghan, S.G, Population Balance Model for Solid State Sintering. Part II. Grain Growth, Ceramics International, 27 (1), (2001) pp 63 - 71.

· M. Subbanna, Pradip and S.G. Malghan, Shear Yield Stress of Flocculated Alumina-Zirconia Mixed Suspensions : Effect of Solid Loading, Composition and Particle Size Distribution, Chem. Engg. Sci, 53(17), (1998) pp 3073-79

· Manjunath Subbanna, Sandhya Kokil, P.C. Kapur, Pradip and S.G. Malghan, An Aggregation Index for Monitoring the State of the Suspensions, Langmuir, 14, (1998) pp 7364-70

· V. Ramakrishnan, Pradip and S.G. Malghan, The Stability of Alumina-Zirconia Suspensions, Colloids and Surfaces, 133, (1998), pp 135-142

· S. Sivakumar, Pradip, P.C. Kapur and S.G. Malghan, Size-interval by Size-interval Marching Algorithm for Simulation of Intermediate Stage of Sintering, Colloids and Surfaces, 133, (1998), pp 173-182

· V. Ramakrishnan, Pradip, S.G. Malghan, Yield Stress of Alumina Zirconia Suspensions, J. American Ceramic Society , 79(10), (1996), 2567-76

· Pradip, R. S. Premachandran and S. G. Malghan, Electrokinetic Behaviour and Dispersion Characteristics of Ceramic Powders with Cationic and Anionic Polyelectrolytes, Bull. of Materials Science, 17(6), (1994), pp 911-920

· Pradip, Design of Crystal-Structure Specific Surfactants Based on Molecular Recognition at Mineral Surfaces, Current Science, 63(4), (1992), pp 180-186.

· Pradip, On the Interpretation of Electrokinetic Behaviour of Chemisorbing Surfactant Systems, Trans. Indian Inst.of Metals, 41(1), (1988), pp 15-25.

